Sol Global Solar           		Sol Global Solar

100% American Made		Technical Sheet 260W Mono PV Module

Material and Assembly

# Greenway GS260WM

#### Warranty						27 years

# Electrical Characteristics

#### Maximum Power (Pmax)  				260 Watt

Power Tolerance  					+3 %

Maximum Power Voltage (Vmp)    		47.65 Volt

Maximum Power Current (lmp)  			5.46 Ampere

Open circuit Voltage (Voc) 				59.20 Volt

Short circuit Current (lsc)  				5.80 Ampere

Maximum System Voltage  			1000 Volt DC

Module Efficiency (ηm)  				16.04 %

Temp. coefficient Voc				 -0.35±0.02 %/℃

Temp. Coefficient Isc   				+0.04±0.0015 %/℃

Temp. Coefficient Power  				 -0.5±0.05 %/℃

Nominal operating cell temperature (NOCT) 	 47°C±2°C ℃

# Cells

Brand Name of Solar Cells  			Greenway

Cell Type  						Mono Crystalline Cell

Cell Size 						5”x 5”

Cell Shape  						Quasi Square

Number Cells   					104 in series

Encapsulated Solar Cells Efficiency (ηc) 		17.5 %

Standard Test Conditions 				UL 1703

Irradiation 1000W/m2 				Tc 25°C

### Mechanical Characteristics

### Dimensions

Length                      				68 1/4”

Width                     				42 3/8”

Depth                       				1.5”

### Installation Dimensions

Length                     				68 3/4”

Width                       				42 7/8”

Weight                                                	45 LB

Frame 				             	Aluminum 45 degree Corners

###### Front side  						Glass Tempered 91% Transmission

Front glass thickness    				1/8”

Encapsulate 						EVA

Back side   						FPE

Junction Box  					Greenway

Absolute Maximum Ratings

Operating Temperature				-40℃～+90℃ ℃

Storage Temperature 				-40℃～+90℃ ℃

Dielectric Isolation Voltage 			1000 VDC max 1000V

Maximum Wind Resistance  			60m/s N/m2 or max Km/h

Maximum Load Capacity 				200 Kg/m2

Maximum Hail diameter @ 				80Km/h  25mm @ 80Km/h

##### Greenway Solar Power

530-903-4804

CEC, Ul 1703, IEC, pending Oct 2010